DWDM 100G Filters

Features ：

High throughput and low loss: The 100G DWDM (Dense Wavelength Division Multiplexing) filter efficiently separates different wavelength signals with minimal loss, suitable for high-speed data transmission.

High wavelength selectivity: It precisely selects wavelengths, minimizing cross-talk between adjacent channels and ensuring system stability.

Wide bandwidth support: It can support up to 100 different wavelengths, meeting the high-density optical communication demands.

Application：

Fiber optic communication

Data centers

Fiber optic access networks

Specification：

| Specification |  |
| --- | --- |
| Operating Wavelength Range (nm) | 1440.0 ~ 1640.0 |
| Center Wavelength*λc (nm) | λc |
| Center Wavelength Tolerance (nm) | λc0.00 ~ +0.30 |
| Passband (-0.25 dB from peak) Wavelength Range λp | ＞0.40，＜0.51 |
| Reflect Band @-30dB Wavelength Range λr | ＜1.20 |
| Insertion Loss @Peak Wavelength Within λp (dB) | ＜0.35 |
| Ripple within passband (dB) | ＜0.25 |
| Reflection isolation within passband (dB) | ＞14 |
| Differences among Passband CWLs@0.5, 3.0 and 25dB down(nm) | ＜0.03 |
| Differences among Passband CWL@0.5dB down and Reflect Band @10dB down(nm) | ＜0.03 |
| Angle of Incidence (degrees) | 1.8° |
| Polarization Dependent Loss within Passband (dB) | ＜0.1 |
| Operating Temperature (°C) | 0 ~ 75 |
| Wavelength Thermal Shifting Δλ/ΔT (nm/°C) | ＜0.0007 |
| Substrate Material | High Quality Optical Glass |
| Dimension (mm) | (1.30~1.43)× (1.30~1.43)×(0.9~1.40) with 0.25°wedge |
| Backside AR Coating | ＜0.2% Reflection |
| *Center wavelength is defined as the center of two -3.0dB down points |  |